## Slide 1
Advanced Mechanics
(Lecture 10)
ANNOUNCE / BUSINESS
HW 4 (due TODAY)
HW 5 (due next week)
NEW STUFF
Fatigue (can still be quasi-static)
Dynamic loading
Impact

## Slide 2
Fatigue
Nature of fracture in ductile metals in fatigue loading is different from that in static loading
  Failure surface shows two zones of failure
    “beach marks” due to gradual crack development
    sudden fracture
http://www.leancrew.com/all-this/2014/01/bridge-failure/
Repeated loading (also “fluctuating” or “alternating” stresses) below ultimate, and even yield, strength may result in reduced strength (and ductility)
Important factors: stress, structural discontinuities, quality of surface finish, chemical nature of environment

## Slide 3
Fatigue
Repeated loading (also “fluctuating” or “alternating” stresses) below ultimate, and even yield, strength may result in reduced strength (and ductility)
Important factors: stress, structural discontinuities, quality of surface finish, chemical nature of environment
Types of fracture in ductile metals in fatigue loading are different from those in static loading
Failure surface shows two zones of failure
  “beach marks” due to gradual crack development
  sudden fracture
http://www.leancrew.com/all-this/2014/01/bridge-failure/

## Slide 4
Fatigue = Progressive Fracture
Fatigue life / strength: number of stress cycles to fracture
  experimentally defined; reported with S-N diagram
fatigue, or endurance, limit
fatigue strength, (“completely reversed”), is not one number, but varies with number of cycles
Origin of fatigue failure is typically a crack … “progressive fracture” is more accurate mechanistic description than “fatigue” (in my opinion! )
Compressive stress believed to not contribute to crack growth

## Slide 5
Fatigue
Every material has a unique S-N curve
Fatigue life is defined as
where

## Slide 6
Fatigue – Mean Stress
Common to have alternating sinusoidal stress imposed on a uniform, or mean, stress
May be due to vibration imposed on a part under stress
Alternating stress is most important to failure, especially if mean stress is negative, but still need to account for both

## Slide 7
Fatigue Life
Mean stress influences S-N behavior
(Dowling, Fig 9.25)

## Slide 8
Fatigue Failure Criteria
Fatigue criteria provide a way to determine the completely reversed () stress, or fatigue strength, for given material properties and combinations of alternating and mean stresses.
good for steel
(not as conservative)
(equivalent to Modified Goodman for brittle materials)
Notes: We see that each equation relates the applied mean and alternating stresses to a completely reversed alternating stress and a failure strength parameter

## Slide 9
Fatigue Life
To make sense of these relationships, plot v. (constant life diagram)
(Dowling, Figs 9.34, 9.36)

## Slide 10
Fatigue
Once we know the fatigue strength for a given loading combination …
we can determine the number of cycles to failure

## Slide 11
Fatigue

## Slide 12
Example
Example 4.7 (modified): A square prismatic bar is subjected to axial tension (). The fatigue strength for completely reversed stress at is , and the static tensile yield strength is . Apply the Soderberg criterion to determine the limiting value of completely reversed moment that will not result in fatigue failure at .
* Note that although mean and alternating stresses were caused by different modes of loading here, this is not generally the case

## Slide 13
Fatigue Failure Criteria – Combined Loads
What about when repeated stress at a location includes contributions from multiple modes of loading?
Use static failure theory approach to find “effective” alternating and mean stress values, e.g., using distortion energy,
Then use these effective stresses in fatigue failure criteria.
Note that the validity of this approach is questionable for loading scenarios where the principal stress directions change as part of the loading. The book says nothing about this limitation, but this is beyond the scope of our class.

## Slide 14
Example
Example 4.8: Consider a thin-walled cylindrical tank of radius and thickness , subject to an internal pressure varying from a value of to . Employ the octahedral shear stress theory together with the Soderberg criterion to compute the value of producing failure after cycles. The material tensile yield strength is and the fatigue strength is at cycles.

## Slide 16
Impact / Dynamic Loading

## Slide 17
Notes: This rigging company is in West Valley City!

## Slide 18
Impact / Dynamic Loading
Forces suddenly applied to parts / structures
Shock or impact loading occur when time of load application is equal to or smaller than largest natural period of vibration of the structure – stress waves are significant